UT Calibration Block

그림	품명 및 규격	적 용
	Calibration Block IIW Type 1 / V1, A2ASTM E164MIL-STD 2154BS2704AWS D1, 0-69, D2.0-69	수직탐상, 사각탐상시 초음파 탐상기의 시간축 및 감도 교정 (입사점, 입사각 측정)*mm or inch 선택?Materials :Aluminum7075-T6Steel A36/1018Stainless Steel 304

	Calibration BlockIIW type 2US Air Force 33B-1-1	수직탐상, 사각탐상시 초음파 탐상기의 시간축 및 감도 교정 (입사점, 입사각 측정)* mm or inch 선택?Materials :Aluminum7075-T6Steel A36/1018Stainless Steel 304

	Miniature Angle Beam BlockV2 / A4 (ROMPAS)ASTM E164BS2704	사각탐상에서 거리, 입사점, 입사각 측정BS2702, ASTM 164* 0.5", 1.0", 20mm(inch or mm)?Materials :Aluminum7075-T6SteelA 1018Stainless Steel 304

	DSC (AWS Type)Distance / Sensitivity BlockASTM E164	사각탐상에서 거리, 입사점, 입사각 측정AWS?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	SC (AWS type)Sensitivity Block	사각탐상에서 초음파탐상기의 감도 측정AWS?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	DS(AWS Type) Distance / Sensitivity bloc	초음파탐상기의 수평 직선성, dB정확도 AWS?Materials : Aluminum7075-T6Steel 1018Stainless Steel 304

	DC (AWS Type)Distance block	사각탐상에서 거리 및 입사점 측정 AWS?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	RC (AWS Type)Resolution block	사각탐상에서 프로브의 분해능 측정(45,60,70)?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	Miniature Resolution Calibration block	Straight Beam, sensitivity,Resolution, distance amplitude correction?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	30FBH Resolution BlockASTM E127, ASTM E428(Hole Dimensions only)	Straight Beam,Sensitivity, resolution, flaw size, Flaw depth?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	NAVSHIPS Calibration BlockMIL-STD-271F(SH)-6-27-86,Navships 0900-006-3010 Sec.6	Distance Correction and Sensitivity?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	ASME N-625 Reference BlockASME Boiler &Pressure VesselCode, Section IIINuclear Vessels, 1965..	Straight beam sensitivityAngle beam. SensitivitySurface Wave Sensitivity?Materials :Aluminum7075-T6Steel 1018Stainless Steel 304

	ASTM AreaAmplitude Block(8)SpecificationsASTM E127, ASTM E428	수직탐상에서 불감대, 감도,거리,반사원의 면적에 따른 증폭 직선성 측정?Materials :Aluminum7075-T6Steel 4340 Vac.MeltStainless Steel 304	1/64" - 3.0" (1-0300)2/64" - 3.0" (2-0300)3/64" - 3.0" (3-0300)4/64" - 3.0" (4-0300)5/64" - 3.0" (5-0300)6/64" - 3.0" (6-0300)7/64" - 3.0" (7-0300)8/64" - 3.0" (8-0300)

	ASTMDistance/Area Amplitude BlockSpecificationsASTM E127, ASTM E428	수직탐상에서 불감대,감도,거리, 반사원의 면적에 따른 증폭 직선성 측정?Materials :Aluminum7075-T6Steel 4340 Vac.MeltStainless Steel 304	3/64" - 3.0" (3-0300)5/64" - .12" (5-0012)5/64" - .25" (5-0025)5/64" - .50" (5-0050)5/64" - .75" (5-0075)5/64" - 1.5" (5-0150)5/64" - 3.0" (5-0300)5/64" - 6.0" (5-0600)8/64" - 3.0" (8-0300)8/64" - 6.0" (8-0600)

	ASTM Distance Amplitude Set(19 block)SpecificationsASTM E127, ASTM E428	수직탐상에서 불감대,감도,거리,반사원의 면적에 따른 증폭 직선성 측정?Materials :Aluminum7075-T6Steel 4340 Vac.MeltStainless Steel 304	Contains hole diameters of 3/64", 5/64" or 8/64" with metal travel distances of :
			.06" -1.25".12" -1.75".25" -2.25".37" -2.75".50" -3.25"	.62" -3.75".75" -4.25".87" -4.75"1.0" -5.25".........5.75"

	ASTM A609Standard Reference BlockBasic Set	16-0100 1 [25] 16-0200 2 [50] 16-0300 3 [75] 16-0600 4 [150] 16-1000 5 [255] 16-B00B

	ASTM A609Dual-Search Unit Calibration2"x2"x10"	Standard Reference BlockFor Dual-Search Unit calibration2" X2"X 10"2.4 mm flot-Bottom Holes 3,6,13,19,25,32,38,44,50

	ASME Basic Calibration Blocks	Weld Thickness t 1 in. or lessOver 1 in. through 2 inOver 2 in. through 4 inOver 4 in. through 6 inOver 6 in. through 8 inOver 8 in. through 10 inOver 10 in.	Basic Calibration Block두께 T3/4 in. or t1-1/2 in. or t3 in. or t5 in. or t7 in. or t9 in. or t1 1 in

	RB-RD BlockKSB 0534	경사각 탐상의 원거리 분해능 측정용?Materials :Aluminum7075-T6Steel 4340Stainless Steel 304

	MU Block	V1 Block을 사용이 간편하도록 기능을 추가하여 특별히 작게 만들어진 BlockMetric Universal Calibration Standard 20X50X150mm ?Materials :Aluminum7075-T6Steel 4340Stainless Steel 304